支持信息

表S1常见的P型有机单晶及其光电性质。

Table S1 P-type organic single crystals and their optoelectronic properties.

| 分子结构式 | 迁移率 (μh = cm2 V-1 s-1) | 荧光发射峰值 (nm) | HOMO/LUMO (eV) | 参考文献 |
| --- | --- | --- | --- | --- |
| Perylene | 0.1 | 447 441 | -5.3/-2.3 | [1] |
| Rubrene | 24.5 | 570 | -5.4/-3.2 | [2] |
| C8-BTBT | 30 | - | - | [3] |
| TIPS-pentacene | 6 | - | - | [4] |
| BP1T-OMe | 0.0076 | - | - | [5] |
| C10-DNTT | 12.5 | - | -5.4/-2.4 | [6] |
| BP1T | 0.0063 | 467/491 | -5.26/-1.57 | [7] |
| BP3T | 1.64 | 575/635 | -5.08/-2.76 | [8] |
| AC5 | 0.022 | 515/550 | -5.16/-1.7 | [9] |
| BP2T | 0.42 | 544 | -4.83/-2.8 | [10] |
| BSB-Me | 0.17 | 456/482/521 | -5.6/-2.7 | [11] |
| Tetracene | 2.3 | 514 | -5.4/-2.4 | [12] |
| Pentacene | 35~40 | 560 | -5.0/-3.2 | [13] |
| DPA | 34 | 441 | -5.6/-2.6 | [14] |
| TPPy | 0.37 | 478 | -5.7/-2.7 | [15] |

表S2常见的N型有机单晶及其光电性质。

Table S2 N-type organic single crystals and their optoelectronic properties.

| 结构式 | 迁移率 (μe = cm2 V-1 s-1) | 荧光发射峰值 (nm) | HOMO/LUMO (eV) | 参考文献 |
| --- | --- | --- | --- | --- |
| F2-TCNQ | 67 | - | - | [16] |
| AC5-CF3 | 1.5 | 504.8/541.4 | -5.51/-2.11 | [17] |
| BPTB | 1.83 | 463/483/513 | -5.63/-2.73 | [18] |
| P2TCF3 | 0.07 | 550/590 | - | [19] |

表S3常见的双极性有机单晶及其光电性质。

Table S3 Ambipolar organic single crystals and their optoelectronic properties.

| 结构式 | 空穴迁移率 (μh = cm2 V-1 s-1) | 电子迁移率 (μe = cm2 V-1 s-1) | 荧光发射峰值 (nm) | HOMO/LUMO (eV) | 参考文献 |
| --- | --- | --- | --- | --- | --- |
| 2-CSB | 0.69 | 0.26 | 490 | -5.7/-2.9 | [20] |
| β-CNDSB | 2.1 | 2.5 | 421/448 | -6.01/-3.26 | [21] |
| dNaAnt | 0.29 | 0.39 | 450 | -5.3/-2.6 | [22] |
| P4V3 | 0.12 | 0.11 | 527 | -5.7/-3.0 | [23] |

参考文献：

[1]	Dresner J. Double injection electroluminescence in anthracene. RCA REVIEW, 1969, 30: 322-&

[2]	Takeya J, Yamagishi M, Tominari Y, et al. Very high-mobility organic single-crystal transistors with in-crystal conduction channels. Appl Phys Lett, 2007, 90: 102120

[3]	Minemawari H, Yamada T, Matsui H, et al. Inkjet printing of single-crystal films. Nature, 2011, 475: 364-367

[4]	Hulea I N, Fratini S, Xie H, et al. Tunable Fröhlich polarons in organic single-crystal transistors. Nat Mater, 2006, 5: 982-986

[5]	Katagiri T, Ota S, Ohira T, et al. Synthesis of thiophene/phenylene co‐oligomers. V. Functionalization at molecular terminals toward optoelectronic device applications. J Heterocycl Chem, 2007, 44: 853-862

[6]	Peng B, Wang Z, Chan P K L. A simulation-assisted solution-processing method for a large-area, high-performance C 10-DNTT organic semiconductor crystal. J Mater Chem C, 2016, 4: 8628-8633

[7]	Hibino R, Nagawa M, Hotta S, et al. Emission Gain‐Narrowing from Melt‐Recrystallized Organic Semiconductors. Adv Mater, 2002, 14: 119-122

[8]	Ichikawa M, Nakamura K, Inoue M, et al. Photopumped laser oscillation and charge-injected luminescence from organic semiconductor single crystals of a thiophene/phenylene co-oligomer. Appl Phys Lett, 2005, 87: 221113

[9]	Kanazawa S, Ichikawa M, Koyama T, et al. Self-Waveguided Photoemission and Lasing of Organic Crystalline Wires Obtained by an Improved Expitaxial Growth Method. ChemPhysChem, 2006, 7: 1881-1884

[10]	Wang Y, Kumashiro R, Li Z, et al. Light emitting ambipolar field-effect transistors of 2,5-bis(4-biphenyl)bithiophene single crystals with anisotropic carrier mobilities. Appl Phys Lett, 2009, 95: 103306

[11]	Nakanotani H, Kabe R, Yahiro M, et al. Blue-light-emitting ambipolar field-effect transistors using an organic single crystal of 1, 4-bis (4-methylstyryl) benzene. Applied physics express, 2008, 1: 0918011-0918013

[12]	Hepp A, Heil H, Weise W, et al. Light-emitting field-effect transistor based on a tetracene thin film. Phys Rev Lett, 2003, 91: 157406

[13]	Jurchescu O D, Popinciuc M, Van Wees B J, et al. Interface‐controlled, high‐mobility organic transistors. Adv Mater, 2007, 19: 688-692

[14]	Liu J, Zhang H, Dong H, et al. High mobility emissive organic semiconductor. Nat Commun, 2015, 6: 10032

[15]	Bisri S Z, Takahashi T, Takenobu T, et al. Ambipolar field-effect transistor of high photoluminescent material tetraphenylpyrene (TPPy) single crystal. Japanese journal of applied physics, 2007, 46: L596-L598

[16]	Krupskaya Y, Gibertini M, Marzari N, et al. Band-Like Electron Transport with Record-High Mobility in the TCNQ Family. Adv Mater, 2015, 27: 2453-2458

[17]	Sengoku T, Yamao T, Hotta S. Organic light-emitting diodes based on layered films of thiophene/phenylene co-oligomers. J Non-Cryst Solids, 2012, 358: 2525-2529

[18]	Siddiqui S A, Al-Hajry A, Al-Assiri M S. Ab initio investigation of 2,2′-bis(4-trifluoromethylphenyl)-5,5′-bithiazole for the design of efficient organic field-effect transistors. Int J Quantum Chem, 2016, 116: 339-345

[19]	Liu L, Yang G, Tang X, et al. The effect of intermolecular interactions on the charge transport properties of thiazole/thiophene-based oligomers with trifluoromethylphenyl. J Mol Graph Model, 2014, 51: 79-85

[20]	Wang H, Sun F, Zhao Y, et al. A highly luminescent organic crystal with the well-balanced charge transport property: The role of cyano-substitution in the terminal phenyl unit of distyrylbenzene. Organic Electronics, 2016, 28: 287-293

[21]	Deng J, Xu Y, Liu L, et al. An ambipolar organic field-effect transistor based on an AIE-active single crystal with a high mobility level of 2.0 cm2 V-1 s-1. Chem Commun, 2016, 52: 2370-2373

[22]	Qin Z, Gao H, Liu J, et al. High‐Efficiency Single‐Component Organic Light‐Emitting Transistors. Adv Mater, 2019, 31: 1903175

[23]	Nakanotani H, Saito M, Nakamura H, et al. Highly balanced ambipolar mobilities with intense electroluminescence in field-effect transistors based on organic single crystal oligo(p-phenylenevinylene) derivatives. Appl Phys Lett, 2009, 95: 033308